Pure Matte

Premium interior wood topcoat that provides a uniform natural appearance while protecting the wood underneath.

* Ultralow sheen matte look
* Excellent chemical and water resistance
* Natural look to the wood protects without increase in gloss

Technical Data

Description: Pure Mate is a low sheen natural looking product that provides Protection to the wood without changing it natural look.

Viscosity: 125 -150 Centipoise

pH: 7.5-8.5

Density: 8.9lbs/gal at 68°F

VOC: <225g/L

Color: white

Gloss: Matte

Coverage: 400-500 square FT

 APPLICATION:

PREPARATION & APPLICATION

Stir well prior to use. Sand sealer coat using a 220 grit sandpaper, this is for best adhesion of top coat. Clean with vacuum and tack cloth. Using a roller or T-bar, apply thin, even coats in the direction of the grain. Finish will be dry and ready to recoat in two hours in normal conditions.